## Slide 1: Superconductivity, Superconducting RF & Superconducting Magnets
J. G. Weisend II

## Slide 2: Goals
Describe the basic physics behind superconductivity (mainly low TC )
Describe the requirements of practical superconducting materials
Describe how superconducting materials are turned into practical conductors for applications
Discuss superconducting magnets including stability, protection and show an example
Discuss superconducting radiofrequency systems (SCRF)
Touch briefly on HiTC superconductivity

## Slide 3: Introduction
As we’ve seen, superconductivity is a major motivating factor for the use of cryogenics – particularly in accelerators but also in commercial systems such as MRI
Cryogenic engineers will frequently be called upon to design systems to cool and keep cold superconducting equipment
Thus, understanding the requirements of superconductors is an important part of the training of a cryogenic engineer.
What is a superconductor?
  A superconductor is a material that conducts DC electrical current with zero resistive losses under certain specific conditions
    When in the superconducting state the resistive loss is identically zero not just vanishingly small but zero

## Slide 4: Discovery of Superconductivity
H. Kamerlingh-Onnes June 9, 1911 – University of Leiden
  Kamerlingh-Onnes had previously been the first to liquefy helium in 1908
  Having liquid helium available enabled this discovery

## Slide 5: Conditions for Superconductivity
Critical Temperature
  All superconductors have a temperature
  above which they no longer
  become superconducting
This is an obvious condition but by no means
the only condition
To understand the other conditions we need
to understand the magnetic properties of
superconductors
Not all materials are superconductors
– most in fact aren’t
From: Helium Cryogenics
Van Sciver

## Slide 6: Superconductors & Magnetism
Superconductors are also perfect diamagnets i.e. they expel all magnetic field (the Meissner effect)
  This is a different result than if we considered the material as a pure conductor
    This is demonstrated by the “floating magnet” trick
If the applied magnetic field exceeds a certain level, the superconductor reverts back to a normal conductor.
Critical Field
  All superconductors have a field above which they become normally conducting

## Slide 7: Superconductors & Magnetism

## Slide 8: Type II Superconductors
Some superconductors have 2 critical fields: below the first (Hc1) all magnetic flux is expelled from the material. Above the first but below the second (Hc2) the flux penetrates in the form of quantized magnetic fields or fluxons. In this “mixed state” the bulk of the material remains superconducting
Such material are called Type II superconductors
Type II materials tend to be alloys though Nb is an important Type II superconductor
Type II superconductors have much (orders of magnitude) higher upper critical fields and thus are more useful in technology

## Slide 9: Type II Superconductors
Type I ( < 1/√2)
Type II ( > 1/√2)
Pure metals
BC ≈ 10-3…10-2 T
Dirty materials: alloys intermetallic, ceramic
BC ≈ 10…102 T
Ginzburg, Landau, Abrikosov, Gor’kov, 1950…1957
Complete field exclusion
Partial field exclusion
Lattice of fluxons

## Slide 10: Fluxons can be directly seen (note similarity to quantized vortices in He II)
Courtesy L. Boturra of CERN
Observation on Pb-4at% In magnetised by a field of 3000 Oe and decorated by Co particles
Essmann & Träuble, 1967
0 = h/2e = 2.07 x 10-15 Wb
Flux quantum
Supercurrent

## Slide 11: Critical Current
A third parameter in superconductivity is critical current. If the critical current is exceed superconductivity breaks down
The current in a superconductor stems from 2 causes. The transport current and the shielding currents required for the Meisser or mixed states. Thus, the critical current and critical fields are related.
If we exceed the critical current ( frequently expressed as critical current density Jc ) critical temperature or critical field the material stops being a superconductor
  We call this “going normal” or Quenching
  Thus the point at which a material is superconducting becomes a 3D space

## Slide 12: LHC NbTi Wire
B [T]
T [K]
Jc [A/mm2]
5
5
100
1,000
10,000
100,000
10
10
15
B = 5 [T]
T=1.9 K
T=4.2 K
Jc (5 T, 4.2 K) ≈ 3000 A/mm2
Note Improvement in B and Jc
@ T = 1.9 K
Courtesy L. Boturra of CERN

## Slide 13: Flux Pining
In Type II superconductors the Lorentz force caused by the interaction between the current and the magnetic field will cause the fluxons to move.
Movement of the fluxons will cause heating and thus quenching of the superconductor
From Engineering Superconductivity
P. Lee

## Slide 14: Flux Pining
In practical superconductors the fluxons are pined to prevent movement – this allows higher current densities.
Pinning sites are created by complicated metallurgical processes (heat treatments, cold work and alloying)
This development over the last 30 years has been a major victory in developing practical superconductors for applications

## Slide 15: Flux Pining Sites
Microstructure of Nb-Ti
Precipitates in alloys
Grain boundaries in
inter-metallic compounds
Microstructure of Nb3Sn
Courtesy L. Boturra of CERN

## Slide 16: But Wait! What Causes Superconductivity?
The following is a very hand waving explanation of the origin of low temperature superconductivity
There is a very elegant, accurate and complicated description of low temperature superconductivity:
  This is the Bardeen-Cooper- Schrieffer theory or BCS theory
Simply put
  Electrons in the material are linked together into Cooper pairs via an attractive force that comes from the oscillations of the (positively charged) lattice
  These Cooper pairs now act more like bosons and in a sense undergo a Bose-Einstein condensation similar to that seen in He II
  This “condensate” in effect acts as one “unit” you can not scatter or change the energy of a single electron without changing the energy of all of them
    There is thus an energy gap and unless the energy of interactions exceeds this value there is no scattering and thus no resistance
BCS theory explains and predicts observable behavior in low Tc superconductors

## Slide 17: Another Way to Model Superconductivity is via the “Two Fluid Model”
This imagines superconducting materials as being composed of two kinds of electrons : Those in Cooper pairs and those not in Cooper pairs
  Above TC there are no Cooper pairs
  At absolute zero all electrons are in Cooper pairs
In DC applications the Cooper pairs carry all the electric current and thus there is zero resistance
But in AC (i.e. RF) applications the oscillating electric field affects both the Cooper pairs & the non paired electrons & the movement of the non paired electrons result in resistance.
  Thus there is always electrical loss in AC superconductivity
A similar model is also used to describe He II

## Slide 18: Impact of Changing Currents
In addition to the intrinsic losses caused by AC currents in superconductors. There are additional AC losses that can be reduced via superconductor design
They are broadly speaking 2 major sources of additional AC losses in superconductors: hysteresis (caused by flux jumping) and losses caused by AC coupling between adjacent filaments.
See Backup slides for additional details

## Slide 19: Practical Superconductors
Superconductors are relatively poor conductors when normal
Superconductors do have resistive losses when the current is varied
Superconductors can’t generally be used as a bulk material. They are divided into filaments (tens of mm in DIA) housed in a good conductor (known as a stabilizer) matrix. This:
  Prevents flux jumping and resultant heating
  Increases stability
Groups of filaments themselves are also twisted into a cable to reduce coupling and resulting AC losses in the cables
AC fields also induce eddy current losses in the good conductor within which the superconducting filaments are housed
The two workhorse practical low Tc superconductors are:
  Nb Ti (ductile)
  Nb3Sn ( higher Jc and Hc but a brittle inter metallic compound)

## Slide 20: Practical Superconductors
It’s important to note that while superconductivity was discovered in 1911, practical high current density superconducting materials were developed until the 1960s and weren’t suitable for wide spread technological applications (understanding flux pining, manufacturing techniques ) until the 1980’s
This has implications for applications using the much more complicated HiTc superconductors
How do we create superconducting wire?

## Slide 21: Nb-Ti manufacturing route
extrusion
cold drawing
heat
treatments
NbTi is a ductile alloy that can sustain large deformations
IC(5 T, 4.2 K) ≈ 1 kA
NbTi billet
Graphics by courtesy of Applied Superconductivity Center at NHMFL
1 mm
LHC wire
slide courtesy of L. Boturra - CERN

## Slide 22: Nb3Sn manufacturing routes
Nb3Sn is brittle and cannot be drawn in final form. The precursors are drawn and only later the wire is heat-treated to ≈650 C, to form the Nb3Sn phase
Graphics by courtesy of Applied Superconductivity Center at NHMFL
IC(12 T, 4.2 K) ≈ 1.5 kA
slide courtesy of L. Boturra - CERN

## Slide 23: Superconducting cables
CICC
Braids for
power transmission
Rutherford
Super-stabilized
Internally cooled
slide courtesy of L. Boturra - CERN

## Slide 24: Superconducting Radio Frequency Cavities
From the 70’s to the 90’s the principle application of superconductivity in particle accelerators was in the area of s/c magnets (Tevatron, HERA, LHC)
Since then, for a variety of reasons ( e.g. technical advances in SRF and the growth of linac applications) the use of SRF cavities for particle acceleration has become increasingly important and in many cases is the primary application of superconductivity & cryogenics in accelerator designs

## Slide 25: He II Cooling in SRF is Very Popular
Name | Location | Purpose | Status (as of June 2023) | Comments
LCLS II | USA | FEL Driver | Operating | TESLA Technology
XFEL | Germany | FEL Driver | Operating | TESLA Technology
FLASH | Germany | FEL Driver | Operating | TESLA Technology
SHINE | China | FEL Driver | Under Construction | TESLA Technology
S3FEL | China | FEL Driver | Under Construction | TESLA Technology
DALS | China | FEL Driver | Proposed | TESLA Technology
CEBAF | USA | Electron Linac for Nuclear Science | Operating | 
SNS | USA | Proton Driver for a spallation neutron source | Operating | 
ESS | Sweden | Proton Linac for a spallation neutron source | Beam on dump in Spring 2025 | 
PIP II | USA | Proton Linac for high energy physics | Under Construction | 
FRIB | USA | Heavy Ion Linac | Operating | 
RAON | South Korea | Heavy Ion Linac | Commissioning | 
ILC | Japan | Electron/Positron Collider for High Energy Physics | Proposed | TESLA Technology
S-DALINAC | Germany | FEL Driver, Nuclear Physics & Accelerator R&D | Operating | Extrapolation of TESLA Technology
CBETA | USA | Test Accelerator | Operating | TESLA Technology
MINERVA | Belgium | Proton Linac for Accelerator Driven Reactor | Under Construction | 
CIADS | China | Proton Linac for ADS | Under Construction | 

## Slide 26: Basics of SRF Cavities
SRF cavities deserve their own lecture. (See lecture 12)
This will be a brief overview of the basics of SRF cavities.
Practical cavity material is pure Niobium
Cavities have beam vacuum on the inside (usually separate from insulation vacuum) and are surrounded and cooled by a bath of saturated LHe
Cavities come in all shapes and frequencies (~ 80 MHz – 3.9 GHz) depending on the accelerator design)

## Slide 27: Examples of SRF Cavities
High Beta
  Typically elliptical in design
From H. Padamsee et al.
Superconducting RF for Accelerators
ILC cavity 1.3 GHz
1 m long – also LCLS II

## Slide 28: Examples of SRF Cavities
From H. Padamsee et al.
Superconducting RF for Accelerators
FRIB Cavities
Low Beta
¼ wave & ½ wave cavities

## Slide 29: Surface Resistance, Frequency and Temperature
The RF surface resistance (which we want to minimize) of a SRF cavity is given by:
The surface resistance goes up with frequency and down with temperature: lower temperature equals less resistance, particularly at higher frequencies
Removing heat at lower temperatures is less thermodynamically efficient, thus there is also an energy cost to be paid for operating at lower temperatures.
What is the optimal temperature?
  Above about 500 – 700 MHz you win by operating below 4.2 K ( typically 1.8 – 2 K)
  At lower frequencies (e,g. 80 MHz) you are better at 4.2 K thermodynamically but there may be other considerations (FRIB)
  Between these limits it’s a fairly broad minimum. Most systems operate ~ 2 K – He II

## Slide 30: Cavity Performance
Two of the main parameters for describing Cavity performance are the accelerating gradient Eacc ( MV/m) and the cavity quality factor Q0
Q0 is defined as the energy stored in the cavity divided by the energy lost in one RF period
  Q0 is related to the surface resistance. The lower the surface resistance the higher the Q0 and the lower the energy deposited into the cavity wall and cryogenic system Thus the higher the Qo the better

## Slide 31: Example of SRF Cavity Performance ESS Double Spoke Cavities

## Slide 32: Cavity Performance Can Be Degraded By a Number of Phenomena
Quenching or thermal break down – normal ( non superconducting) zones develop in the cavity
Field Emission – electrons are pulled off the surface of the cavity and accelerated by the RF field (degrades Q0)
Local Magnetic Fields

## Slide 33: Cavity Processing
Research has shown that both Field Emission and Thermal Breakdown can be significantly reduced by proper processing of the cavities. This processing consists of an intricate set of steps involving:
  Cavity surface cleaning by chemicals (buffered chemical processing) or by electropolishing
  Cavity surface cleaning by High Pressure Rising with ultrapure water
  Various heat treatments
Major progress in this area has made SRF cavities much more useful
  CEBAF ( 1980’s) designed for 5 MV/m (actual performance was better) CEBAF 12 GeV upgrade (2000’s) specified & met 19.2 MV/m
  ILC cavity specification is 35 MV/m

## Slide 34: Cavity Cleanliness
Once processed, the RF surface i.e. the beam vacuum surface of the cavities must be kept extremely clean to maintain performance. This results in:
  Assembly of cavity strings in cleanrooms
  Connection of beam tube vacuums within local cleanrooms during cryomodule installation
  Very strict vacuum and particle free requirements for cavity systems
  Presence of fast acting valves to subdivide beam vacuum in the case of accidents

## Slide 35: Other Aspects of SRF Cavities
Q Disease – related to interstitial hydrogen in the niobium.
  Can be treated via heat treatments or may set limits on cavity cool down and warm up rates
Local magnetic fields ( including the Earth’s) degrade cavity performance
  Result is that cavities are designed with passive and sometimes active magnetic shields. Use of magnetic materials near cavities must be carefully examined
Cavities are resonant structures that require tuning frequently at cryogenic temperatures

## Slide 36: Other Aspects of SRF Cavities
Vibrations (microphonics) can detune cavities depending on cavity stiffness and design
  This may put strict limits on vibrations near cavities
  Use of He II ( see later lecture) prevents bulk boiling in the helium bath that may affect the cavity tune

## Slide 37: High Temperature Superconductivity
First Discovered in 1986 in Yttrium Barium Copper Oxide
(YBa2Cu3O7-x), referred to commonly as YBCO - Tc ~92 K
Many other similar ceramic materials soon followed such as Bi2Sr2Ca2Cu3O6 (Bi-2223) – Tc ~ 110 K and HgBa2Ca2Cu3O8 (Hg-1223) – Tc ~ 134 K
This lead to the so-called “Woodstock of Physics” at the 1987 APS March Meeting in NYC
Despite the initial excitement technical progress has been slow and HiTc superconductors have a number of issues:
  While the Tc is high the critical current was (at least initially) is quite low
  These materials are anisotropic (performance depends on their orientation)
  These materials are brittle ceramics and thus very hard to turn into wires
  BCS theory doesn’t explain the presence of superconductivity in these materials – no good theory exists though some type of coherent phenomena must be behind it.

## Slide 38: High Temperature Superconductivity
But don’t despair !
  Remember superconductivity was discovered in 1911 but practical low Tc superconductors really didn’t arrive until the 80’s
There are commercial niche applications of HiTc superconductors even today
HiTc current leads for providing current to low Tc s/c magnets
  These leads allow superconductivity up to about 50 – 80 K and serve to reduce the overall heat leak into the LHe space since HiTc materials are poor thermal conductors
Superconducting electronics in the form of low noise microwave filters for use in cell phone towers operating at about 50 K
Note also the temperature range for HiTc superconductors ( ~ 50 – 200 K ) ties in nicely with the performance range for small cryocoolers
  The development of small cryocoolers and rise of HTS applications have gone hand in hand

## Slide 39: High Temperature Superconductivity Binary Current Leads
From Choi et al.
Adv. Cryo. Engr. Vol 55 (2010)

## Slide 40: Use of HTS Microwave Filters in Cell Phone Base Stations
Courtesy R. Radebaugh

## Slide 41: Stability of Superconducting Magnets
When a wire in a s/c magnet undergoes a temperature rise, there are 2 possibilities:
  It can cool back down and remain superconducting
  It can warm up above Tc and “quench” (become normally conducting in all or most of the magnet)
Which one occurs depends on the amount of heat generation and cooling

## Slide 42: A Genaric Temperature Transient
heat pulse…
…effect of heat conduction and cooling…
generation>cooling
unstable
generation<cooling
stable

## Slide 43: Perturbation spectrum
mechanical events
    wire motion under Lorentz force, micro-slips
    winding deformations
    failures (at insulation bonding, material yeld)
electromagnetic events
    flux-jumps (important for large filaments, old story !)
    AC loss (most magnet types)
    current sharing in cables through distribution/redistribution
thermal events
    current leads, instrumentation wires
    heat leaks through thermal insulation, degraded cooling
nuclear events
    particle showers in particle accelerator magnets
    neutron flux in fusion experiments, separator magnets
slide courtesy of L. Boturra - CERN

## Slide 44: Current Sharing
T
Iop
Top
IC
TCS
T < Tcs
T > Tc
quenched
Tcs < T < Tc
curent sharing
stabilizer
superconductor
stabilizer
superconductor
TC

## Slide 45: Stability of Superconducting Magnets
Fully cryostable: magnet will recover regardless of size of normal zone ( disturbance) May be true of large detector magnets e.g BaBar detector or MRI magnets, but generally magnets are conditionally stable up to some heat input level.
Adiabatic stability: magnet will recover if heat input is not too big – more typical of accelerator magnets or potted-coil magnets

## Slide 46: Stability of Superconducting Magnets(2)
Why not make all magnets fully cryostable?
S800 dipole coil
A1900 dipole coil
S800 dipole coil took 6 weeks to wind
A1900 dipole coil took 2 days

## Slide 47: Criteria for Fully Cryostable Magnets
Stekley Criteria – most conservative, doesn’t account for end cooling
< 1 magnet is stable
Equal area theorem
  Takes into account the cooling of the conductor via conduction at the ends
  Can be expressed as a graphical solution comparing the areas under the cooling and heating curves ( see references )
There are many cooling options for S/C magnets and SRF cavities – see lecture 15

## Slide 48: Quench Detection & Protection
Superconducting magnets store large amounts of energy either individually (20 MJ for the Babar detector magnet) or connected in series (10’s of GJ)
If all the energy is deposited in a small volume, bad things happen!

## Slide 49: Quench Detection & Protection
The goal is to rapidly and accurately detect the quench and safely dispose of the energy
  Spread throughout the magnet
  In an external dump resistor
  In a coupled secondary
  In magnet strings, bypass the energy of the other s/c magnets away from the quenching one
Remember it’s the stored energy in the magnet(s) not the power supply that’s problem (S/C magnet power supplies are low voltage, high current, so increased resistance in a quenched magnet prevent further power input)

## Slide 50: Detecting Quenches
Can’t just measure voltage directly as magnet ramping causes voltage and give a false signal
The general approach is to subdivide the magnet with voltage taps and build a bridge circuit that cancels out voltage due to ramping
Redundant QD systems are necessary
Other measurements such as temperature, helium level or vacuum level might be used to look for precursors to trouble but take care not to “over interlock the magnet”
HTS magnets are of special concern due to slow quench propagation, so sensitive QD required

## Slide 51: Strategy: energy dump
B.J. Maddock, G.B. James, Proc. Inst. Electr. Eng., 115, 543, 1968
slide courtesy of L. Boturra - CERN

## Slide 52: Strategy: heaters
the quench is spread actively by firing heaters embedded in the winding pack, or in close vicinity to the conductor
heaters are mandatory in:
  high performance, aggressive, cost-effective and highly optimized magnet designs (high current density)…
  …when you are really desperate
advantages:
  homogeneous spread of the magnetic energy withn the winding pack
disadvantages:
  active
  high voltages at the heater
  Doesn’t work well with highly stable magnets
winding
heater
slide courtesy of L. Boturra - CERN

## Slide 53: Magnet strings
magnet strings (e.g. accelerator magnets, fusion magnetic systems) have exceedingly large stored energy (10’s of GJ):
    energy dump takes very long time (10…100 s)
    the magnet string is subdivided and each magnet is by-passed by a diode (or thyristor)
    the diode acts as a shunt during the discharge
M1
M2
M3
MN

## Slide 54: Example #1 LHC Dipole
Bnominal 8.3 (T)
current 11850 (A)
stored energy  8 (MJ)
cold mass  35 (tonnes)
slide courtesy of L. Boturra - CERN

## Slide 55: LHC dipole coils
B
B
slide courtesy of L. Boturra - CERN

## Slide 56: Coil winding
B
B
Cable insulation
Coil winding machine
Stored coils
10 m precision !
slide courtesy of L. Boturra - CERN

## Slide 57: Collaring and yoking
175 tons/m
85 tons/m
F
yoking
collaring
slide courtesy of L. Boturra - CERN

## Slide 58: Cold mass
slide courtesy of L. Boturra - CERN

## Slide 59: Cryostat
Low conduction foot
Thermal screens
MLI

## Slide 60: Finally, in the tunnel !
slide courtesy of L. Boturra - CERN

## Slide 61: Example #2 BaBar Detector S/C Solenoid
Provided background field for particle identification for the BaBar detector at SLAC
Physics requirements dictated a relatively thin solenoid

## Slide 62: Properties of BaBar Solenoid
Field: 1.5 Tesla
Stored Energy: 27 MJ
Operating Current: 4596A
Tc= 8.3K
Operating Temp: 4.5K
Total Heat Load at 4.5K: 225liquid-liters/hr
Cryogenics: indirectly cooled using the force flow technique where the liquid He is circulated in cooling pipes welded to the outside diameter of the support tube
Uses NbTi highly stabilized by a pure Al conductor

## Slide 63: BaBar Detector Under Construction

## Slide 64: BaBar Detector

## Slide 65: BaBar Solenoid
Operated almost continuously for ~ 10 years
Was very stable – only discharged due to loss of power, controls or cooling
  Availability was > 96% from the start and better than 98% during final 3 years
    Improvement due mainly to removing unnecessary interlocks and adding additional utility backups

## Slide 66: Conclusions
Superconducting magnets & SRF Cavities make possible modern accelerators : LHC, ILC, ESS, FAIR, SNS, JLAB, LCLS II
Superconducting magnet design involves detailed engineering on a scale from the microscopic (flux pinning) to the immense (multi ton, GJ magnets)
Superconducting magnet design involves a wide range of disciplines: materials science, electrical engineering, mechanical design, cryogenics etc.
Superconducting magnet requirements have driven and enabled many advances in s/c materials, wire and ancillary systems
HTS are still under development but significant niche markets are appearing

## Slide 67: Back Up Slides

## Slide 68: Flux Jumps
slide courtesy of L. Boturra - CERN
DQ
DT
Df
JC
Unstable behavior is shown by all superconductors when subjected to a magnetic field:
  B induces screening currents, flowing at critical density JC
  A change in screening currents allows flux to move into the superconductor
  The flux motion dissipates energy
  The energy dissipation causes local temperature rise
  JC density falls with increasing temperature
Flux jumping is cured by making superconductor in the form of fine filaments. This weakens the effect of  on Q

## Slide 69: Filaments coupling
All superconducting wires and are twisted to decouple the filaments and reduce the magnitude of eddy currents and associated loss
dB/dt
loose twist
dB/dt
tight twist
slide courtesy of L. Boturra - CERN

## Slide 70: Coupling in cables
 dB/dt
cross-over contact Rc
eddy current loop
+I
I
The strands in a cable are coupled (as the filaments in a strand). To decouple them we require to twist (transpose) the cable and to control the contact resistances
slide courtesy of L. Boturra - CERN